### Research Background

### In concrete engineering, designing a mix involves proportioning fine and coarse aggregates, cementitious materials, and water to meet specific performance criteria like workability, strength, and durability. State DOT specifications define these classes to standardize construction for varying environments, from high-traffic pavements to structural bridge components.

### 1. Class 47BD Concrete (Bridge Decks)

This mix is specifically designed for bridge decks, featuring a higher cementitious material content and a lower water-to-cement ratio to increase durability and reduce permeability.

- Total Cementitious Materials: 658 lb/yd³ (minimum).

- Total Aggregate: 2,500 lb/yd³ (minimum) to 3,000 lb/yd³ (maximum).

- Air Content: 6.5% to 9.0%.

- Maximum Water/Cement Ratio: 0.42 lb/lb (typical NDOT standard for 47BD).

- Minimum Required Strength: 4,000 psi (at 28 days).

- Common Use: Bridge decks and bridge approach slabs.

- Reference: NDOT 2017 Standard Specifications Table 1002.02.

### 2. Class 47B-HE Concrete (High Early Strength)

This mix is used when rapid strength gain is required, such as pavement repairs or intersections that need to be opened to traffic quickly.

- Total Cementitious Materials: 752 lb/yd³ (minimum).

- Total Aggregate: 2,500 lb/yd³ (minimum) to 3,000 lb/yd³ (maximum).

- Air Content: 6.5% to 9.0%.

- Maximum Water/Cement Ratio: 0.40 lb/lb.

- Minimum Required Strength: 3,500 psi (typically required in as little as 48 hours depending on project needs).

- Common Use: Rapid-entry pavement repairs and "High Early" strength applications.

- Reference: Nebraska DOT (2017) Standard Specifications, Section 706 (Concrete Bridge Floors) and Table 1002.02

### 3. Iowa DOT Class C (Structural & Paving)

Iowa's primary structural mix used for highway paving and box culverts.

- Total Cementitious Materials: 611 lb/cy (approximate based on standard Iowa 50/50 split).

- Total Aggregate: ~3,100 lb/cy (total combined dry weight).

- Target Air Content: 6.5% (± 1.5%).

- Maximum Water/Cement (w/c) Ratio: 0.488 lb/lb (Target typically 0.43).

- Minimum Required Strength: 4,000 psi (at 28 days).

- Reference: Iowa DOT Standard Specifications Section 2403.

### 4. Colorado DOT (CDOT) Class D (Structural)

A high-density mix used for bridge decks, rails, and structural elements requiring higher strength.

- Total Cementitious Materials: 615 lb/cy (minimum).

- Total Aggregate: ~3,000 lb/cy (total dry weight).

- Target Air Content: 5.0% to 8.0%.

- Maximum Water/Cement (w/c) Ratio: 0.44 lb/lb.

- Minimum Required Strength: 4,500 psi.

- Reference: CDOT 2023 Standard Specifications Section 601, Table 601-1.

Table 1. Summary of Input Parameters for Four Selected DOT Concrete Mix Designs

| Input Parameter | NDOT 47B | NDOT 47BD | Iowa Class C | CDOT Class D |
| --- | --- | --- | --- | --- |
| Cement (lb/cy) | 564 | 658 | 611 | 615 |
| Max w/c Ratio | 0.45 | 0.42 | 0.488 | 0.44 |
| Air Content (%) | 5.0–7.5% | 5.0–7.5% | 5.0–8.0% | 5.0–8.0% |
| Min. Strength (psi) | 3,500 | 4,000 | 4,000 | 4,500 |
| Primary Usage | Pavement | Bridge Decks | Culverts | Dense Bridge Elements |

References

Colorado Department of Transportation. (2023). Standard specifications for road and bridge construction: 2023 specs book (943 pp.). https://www.codot.gov/business/designsupport/cdot-construction-specifications/2023-construction-specifications/2023-specs-book/2023-cdot-specs-book.pdf

Iowa Department of Transportation. (2012). Section 2403: Structural concrete (Standard Specifications for Highway and Bridge Construction, Series 2012). https://ia.iowadot.gov/erl/archiveoct2012/GS/content/2403.pdf

Nebraska Department of Transportation. (2017). Standard specifications for highway construction: 2017 edition (Spec Book). Nebraska Department of Transportation. https://dot.nebraska.gov/media/g4qp4y0d/2017-specbook.pdf